## Slide 1
Beneficial uses of dredged sediments from waterways: Towards a validation step of sediments as a resource
Avec le soutien du Fonds européen de développement régional
ENERO: June 2022
Notes: Interreg et le partenariat transfrontalier France Wallonie Flandre
New cross-border resources: Towards a validation of scenarios for the valorisation of sediments and other materials

## Slide 2: Context: Why VALSE?
General objectives:
Promote the beneficial re-use of soil and dredged materials into the circular economy
Validate cross-border materials valorisation pathways
3 regions with a lack of efficient, operational and sustainable solutions to manage sediments from waterways
3 regions with industrial wastelands / brownfields sites for soil rehabilitation

## Slide 3: Main addressed topics
Legislation analysis (3 regions):
  Law comparison relative to dredged sediments and soil excavation ;
  Identification of restrictions for re-use and valorisation;
  Proposal strength  ease implementation pathway of valorisation.
Tool development :
  Analytical tools for sediments characterization in the field (pXRF, Raman, FTIR, passif samplers, electrodes,…) micro-pollutants
  Decision support tools:
    Models that allow, from the characteristics of sediments, to predict their evolution, their aging as well as potential ways of valorisation;
    Interactive maps which, based on the location of sediments and their physico-chemical characteristics, offer potential ways of valorisation in compliance with the principles of the circular economy.
Exploration of valorisation pathway :
  « Soft » valorisation : Landscaping pathway: sediment mound along a roadside
  « Hard » valorisation : Civil engineering pathway :
    Pouzzolan (sediment fine fraction < 63µm);
    Concrete (raw sediment fraction).

## Slide 4
Aim:
Monitoring of the ecological quality (faunistic and floristic inventories) and the ecotoxicity of materials
Landscaping mound (1)
Volume of unpolluted dredging material: 1500 m³

## Slide 5
Landscaping mound (2)
Landscaping mound and control site (Farciennes, Belgium)
Conclusions:
The use of non-contaminated sediments in a landscaping mount does not have any significant toxic effect on the flora and fauna of Eutrophic sites
Biodiversity index is similar compared to the roadside of the surrounding area with some difference in the fauna species and flora from seeds trapped in the sediments
Eisenia fetida
Origanum vulgare
(June 2020)
Macro-invertebrate sampling
(June 2020)
Floristic inventory
Faunistic inventory

## Slide 6
Pozzolan pathway
Fraction < 63 µm
Drying (70-140°C)
Calcination (750-850°C)
Grinding
(Clinker)
Aim: To assess the potential for valorisation of a river sediment: contribution of the fine fraction (< 63µm) to the pozzolanic cement composition
Process
Pozzolanic reactivity:
All calcinated products are considered reactive
Faster contribution than reference fly ash

## Slide 7
Inventaire floristique
Inventaire faunistique
Conclusion: The equivalent performance and the environmental compatibility demonstrated in the VALSE project present a favorable balance for the pozzolan pathway
Cement
  30% substitution of Portland clinker by calcinated sediments
Performance properties
  Mechanical resistance slightly higher than CEM II/B-V (containing fly ash)
  No setting delay problems, nor affected resistance (combustion of the OM)
  Easily adjustable workability using commercial superplasticizers (PCE type) – Durability (on concrete) has been demonstrated to be equivalent to CEM II/B-V composite cement
Environnemental compatibility
  Leaching (lixiviation) tests on hardened (28 days) and crushed mortars
  No exceeding of the standards observed, heavy metals (if present) are frozen by the cement matrix
Pozzolan pathway

## Slide 8
 | Solid (mg.kg-1) | Eluate (mg.kg-1)
Zn | 1115 | <1
Pb | 194 | <0,5
Cu | 81 | <1
Concrete pathway
Inventaire floristique
Inventaire faunistique
Sediment typology of Hauts-de-France (France) and walloon (Belgium):
  Very high fines (silt) content (70 ─ 90%) → very small grain fraction
  High content of organic matter and heavy metals (mainly: Zn, Pb, Cu) due to a fairly similar industrial history  Contaminated sediments
<63μm | 75%
LOI550°C (≈MO) | 13%
Fluorine >TS : Catégory B (AGW95) | 
Aim: To assess the potential of waterways sediments as a substitute for the sandy fraction in the cement concrete for the construction of a cycle path
Mechanical treatment
Final granulometry
Heavy metal concentrations

## Slide 9
Mechanical performance in test tubes (Φ11*22cm3)
Compression
Splitting
Applicable and current standards:
● NF EN 206
● NF P 98-170 (road cement concrete)
B35 - 28 days :
RC = 23,67 ± 0,96 MPa → C25
RS = 2,73 ± 0,04 MPa → S2,7
→ Concrete of class 5 : sufficient “resistance” for a cycle path
B35 : Sed 220 kg.m-3
Concrete pathway

## Slide 10
 |  | E/C | RC-7 (MPa) | RC-28 (MPa) |  | RS-7 (MPa) | RS-28 (MPa)
Concrete plant | BC1 | 0,53 | 24,83 | 40,11 |  | 2,57 | 3,87
 | BE2 | 0,75 | 14,00 | 26,21 |  | 1,54 | 2,61
Core (cycle path) | BC | 0,53 | 21,54 | 35,06 |  | ─ | 2,01
 | BE | 0,75 | 13,70 | 22,50 |  | ─ | 1,83
1BC = Control concrete; 2BE = B35 = Experimental concrete (35% sand)
From « laboratory » scale to « field» scale : mechanical monitoring of the cyle path
Conclusions:
« Drying delay » effect on BE (concrete with sediment) → sediments affect the rise in resistance due to the negative effect of organic matter on the cement setting;
Labo/Field (Core worksite) → simillar and consistent results.
Concrete pathway
B35 : Sed 220 kg.m-3
Compression
Splitting
Notes: JE NE COMPRENDS PAS CE QU’EST « LE CENTRALE » ET LA CAROTTE

## Slide 11
Concrete pathway
Inventaire floristique
Inventaire faunistique
Conclusions:
1st Educational cycle path with sandy fraction substituted at 35% by mass by contaminated river sediment
Experimental formulation allows the use of 220 kg of dry sediment per m3 of fresh concrete.
“Freezing/defreezing” resistance on BE/BC results show no significant difference
The environmental analysis (lixiviation test) on the concrete leachates comply with the legislation
Pilot test site in Chatelet (Belgium) for the cycle track
Notes: Tu peux t’arreter ici et aller à la conclusion ou ajouter 2 / 3 dia de ton travail. Avec un titre qui pourrait être : « si on veut aller plus loin » et rebondir sur les outils présentés au début de l’exposé… Par contre il faut vraiment rester sur 2/3 dia pas plus ça ne doit pas prendre le dessus.
OK

## Slide 12
Objectives: Characterize the sediments into categories towards the different valoraisation pathways
Approach: Statistical analysis (cluster analysis ) of the Walloon (SPW) and French (VNF) databases, mapping of associations
Sediments classification
Data: inorganic/
organic contaminants, particle size, mineral composition
Notes: A revoir sans doute ou mm à supprimer? CEST BON QUAND MEME

## Slide 13
Interactive map
Strategy proposal : cartographic and GIS tool
Tool: Geographic Information System as a management tool
GIS?
Sensitivity to erosion of agricultural plots on bare soil in Wallonia. Source: Giser
Objective: Interconnection of dredged sediments disposal sites and sites for valorisation pathways

## Slide 14
Relationship between the demand and the offer : From the “disposal sites” towards the “valorisation pathways”
A civil engineer perspective of noise-reducing embankments on motorways
Region of Mons-Charleroi: location of noise-reducing embakments available (Orange dots) along the speeedways on a maximal distance by truck of 10 Km (yellow color area) and of 25Km from a disposal site located at Obourg (green color area). Orange /red stars: disposal sites
Interactive map (1)

## Slide 15
Relationship between the demand and the offer: From the “valorisation pathways” towards the “disposal sites”
An agronomic perspective of valorisation based on flat mining heap
Région Mons-Charleroi: location 25Km from a disposal site available on a maximal distance by road (Yellow color) and of 25Km by truck from a mine heap located in Morlanwelz. Red spots : Contaminated or potentially contaminated soil; Black color: uncontaminated soil; Orange /red stars: disposal sites
Interactive map (2)

## Slide 16
General conclusions
Inventaire floristique
Inventaire faunistique
Promising valorisation pathways of dredged sediments within the circular economy framework with industrial interest for concrete and pozzolan tracks;
1st Walloon educational cycle path based on waterway sediments;
Landscaping mound opportunities (with noise reduction effect);
GIS tool to assist sediment management.
Notes: Tu peux t’arreter ici ou ajouter 2 / 3 dia de ton travail. Avec un titre qui pourrait être : « si on veut aller plus loin » et rebondir sur les outils présentés au début de l’exposé… Par contre il faut vraiment rester sur 2/3 dia pas plus ça ne doit pas prendre le dessus syr.
JE PENSE QUE SI J’AJOUTE DES DIAPOS, CELA DEVIENDRA TROP LONG. MERCI LAURENCE.

## Slide 17: Thank you for your attention
Beneficial Uses of dredged sediments from waterways: Towards a validation step of sediments as a resource
Avec le soutien du Fonds européen de développement régional
www.valse.info